## Slide 1: QXU4004 Eng. Chemistry
Dr Sulafudin Vukusic s.vukusic@qmul.ac.uk

## Slide 2: Week 6: Applications of Molecular Orbital Theory in Materials
Semiconductors

## Slide 3: Suggested Reading List:
Chapter 12 (Section 12.4 “Metallic bonding”, pages 530- 533; Section 12.7 Especially “Semiconductors” and “Semiconductor Doping” pages 539-544): Brown et al.
Chemistry the central science,14th int Ed, Pearson /
ISBN:978-1-292-02152-2

## Slide 4
iii iv v vi
ii
Group II
Group III
Group IV
Group V
Group VI
Candidate Materials - Group III-V & Group II-VI
An example – CdTe, GaP

## Slide 5
Al Ga In
N P
As
AlN, AlP,AlAs GaN, GaP, GaAs InN, InP, InAs
GaAs
GaP
GaAl
GaAsP
GaAsAl
Ternary compounds
Binary compounds
Some examples…
Nomenclature: most electronegative atom considered “charged negatively” and less electronegative “charged positively” (this does not follow reality, it is an assumption just for naming the compound): THEREFORE, named like traditional salts (traditional salts LiF: lithium fluoride OR NaCl: sodium chloride NOTE: NaCl or LiF are NOT semiconductors: they are ionic solids, typical ionic salts. I have just used them here as an example of how to name these compound semiconductors: for example: AlN : aluminium nitride

## Slide 6: Band Theory for Metals (and Other Solids)
There are two broad categories of semiconductors:
  Intrinsic Semiconductors（本征半导体）
    Naturally have a moderate band gap. A small fraction of the electrons in the valence band can be excited into the conduction band. They can carry current.
    The “holes” these electrons leave in the valence band can also carry current as other electrons in the valence band can be excited into them.
  Extrinsic Semiconductors（非本征半导体）
    Have had impurities added in order to increase the amount of current they can conduct. (impurities called dopants（掺杂物）; process called doping)
    The dopants can *either* provide extra electrons *or* provide extra holes:
      A semiconductor doped to have extra electrons is an n-type semiconductor (‘n’ is for ‘negative’)
      A semiconductor doped to have extra holes is a p-type
semiconductor (‘p’ is for ‘positive’)
Notes: n and p type Semiconductor

## Slide 7
Intrinsic semiconductors

## Slide 8
Intrinsic semiconductors – temperature dependence

## Slide 9
Intrinsic semiconductors – temperature dependence

## Slide 10
Intrinsic semiconductors – temperature dependence

## Slide 11
Intrinsic semiconductors – temperature dependence

## Slide 12
Extrinsic semiconductors
Donors: P, As, Sb
Acceptors: B, Al, Ga, In
By substituting a Si atom with a special impurity atom (Column V
or Column III element), a conduction electron or hole is created.

## Slide 13
How does an n-type semiconductor work?
e.g. silicon ([Ne] 3s 2 3p 2) is doped with phosphorus ([Ne] 3s 2 3p 3)
  In silicon, the valence band is completely full and the conduction band is completely empty.
  The phosphorus provides an additional band full of electrons that is higher in energy than the valence band of silicon. Electrons in this donor band are more easily excited into the conduction band (compared to electrons in the valence band of silicon).
Band Theory for Metals (and Other Solids)

## Slide 14
How does a p-type semiconductor work?
e.g. silicon ([Ne] 3s 2 3p 2) is doped with aluminium ([Ne] 3s 2 3p 1)
  In silicon, the valence band is completely full and the conduction
band is completely empty.
  The aluminium provides an additional empty band that is lower in energy than the conduction band of silicon. Electrons in the valence band of silicon are more easily excited into this acceptor band (compared to the conduction band of silicon).
Band Theory for Metals (and Other Solids)

## Slide 15
Donor / Acceptor Levels (Band Model)
Ec
Donor Level
Acceptor Level
ED
EA
Ev
Ionization energy of selected donors and acceptors in silicon
Donor ionization energy
Acceptor ionization energy
 | Donors |  |  | Acceptors |  | 
Dopant | Sb | P | As | B | Al | In
Ionization energy, E c-E d or E a -E v (meV) | 39 | 45 | 54 | 45 | 67 | 160
Ec : Energy of Conduction Band of semiconductor ED : Energy of Valence band of DONOR dopant
EA : Energy of Conduction band of ACCEPTOR dopant
EV : Energy of Valence Band of semiconductor

## Slide 16: Terminology
donor: impurity atom that increases n
acceptor: impurity atom that increases p
n-type material: contains more electrons than holes p-type material: contains more holes than electrons
majority carrier: the most abundant carrier minority carrier: the least abundant carrier
intrinsic semiconductor: n = p = ni
extrinsic semiconductor: doped semiconductor

## Slide 17
The band gap energy is the energy required to free an electron
from a covalent bond.
  EG for Si at 300K = 1.12eV
  Insulators have large EG; semiconductors have small EG
Dopants in Si:
  Reside on lattice sites (substituting for Si)
  Group-V elements contribute conduction electrons, and are called donors
  Group-III elements contribute holes, and are called acceptors
  Very low ionization energies (<50 meV)
 ionized at room temperature
Dopant concentrations typically range from 1014 cm-3 to 1020 cm-3
Some numbers…

## Slide 18: More typically simplified to show only “frontier” bands:
conduction band
Fermi level f
valence band
Metallic Conductor
Insulator
Semi Conductor
Large Band Gap
small band gap
no band gap
E < 10 kJ/mol
E ~ 10 -100 kJ/mol
E > 400 kJ/mol

f

f

## Slide 19: How Defects Improve Semi-Conduction
Pure Germanium
E ~ 0.66 eV
Gallium-Doped Ge
small band gap
Ga more Electropositive:
Adds “Orbitals” At Higher Energy
With Fewer
Electrons
Pure Ge Band Gap
Gallium-Doping creates positive holes, as an acceptor band:
A p-type semi-conductor

## Slide 20: How Defects Improve Semi-Conduction
Pure Germanium
E = 0.66 eV
Arsenic-Doped Ge
small band gap
As is more Electronegative:
Adds “Orbitals” At Lower Energy Partially Filled with Electrons
Pure Ge Band Gap
Arsenic-Doping creates negative holes, as a donor band
An n-type semi-conductor